# HINDUSTAN PETROLEUM CORPORATION LIMITED

(A Government of India Enterprise)

QUALITY CONTROL LABORATORY

MAZGAON TERMINAL

LUBE PLANT, HAY BUNDER ROAD, MAZGAON MUMBAI,400033

# LABORATORY TEST REPORT

ENKLO 46 210 L DRUM HDPE(0235008)

Date

30/06/23

| Laboratory Serial No. | FB - 340 | Sample Drawn By | QC OFFICER |
| --- | --- | --- | --- |
| JDE Serial No | 1250545 | Date Sample Drawn | 16/06/23 |
| Batch No / Lot No | SI-23-F-476 | Date Received In Lab | 16/06/23 |
| Work Order No | 1061349 | Date Tested | 17/06/23 |
| Tank /Kettle/Location | WHS | Particular of Sample | DRUM |
| Plant Code/ Name |  | Sampling Plan | IS 1447 |

Test Line Number

Test Description/ Characteristics

Specifications

Units	Test Method	Min	Max	Result Value

| 17 |  | ZINC CONTENT |  | %Wt |  | ASTM D6443, EDTA |  | .026 |  | .070 |  | .029 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 |  | ACIDITY TOTAL |  | mg KOH/g |  | IS1448(P2),ASTM D664, D974 |  | - |  | 1.50 |  | .45 |
| 2 |  | APPEARANCE |  | . |  | VISUAL |  | B&C |  | B&C |  | B&C |
| 3 |  | EMULSION CHAR @54°C/ 20MIN |  | Milliliter |  | IS1448(P91),ASTM D1401 |  | 40-40-0 |  | 40-37-3 |  | 40-38-2 |
| 4 |  | POUR POINT, °C |  | °C |  | IS1448(P10), ASTM D97 |  | - |  | -3 |  | -9 |
| 5 |  | VISCOSITY INDEX |  | . |  | IS1448(P56), ASTM D2270 |  | 90 |  | - |  | 99 |
| 15 |  | DENSITY@29.5°C |  | g/cc |  | IS1448P16,ASTMD1298,D4052D7042 |  | - |  | - |  | .8756 |
| 6 |  | K V @ 100°C |  | cSt |  | IS1448(P25), ASTM D445, D7042 |  | - |  | - |  | 6.560 |
| 7 |  | K V @ 40°C |  | cSt |  | IS1448(P25), ASTM D445, D7042 |  | 42.00 |  | 50.00 |  | 43.96 |
| 8 |  | FLASH POINT,COC |  | °C |  | IS1448(P69), ASTM D92 |  | 190 |  | - |  | 236 |
| 9 |  | FOAMING STABILITY SEQ1 |  | Milliliter |  | IS1448(P67), ASTM D892 |  | 0 |  | 0 |  | 0 |
| 10 |  | FOAMING STABILITY SEQ2 |  | Milliliter |  | IS1448 (P67),ASTM D892 |  | 0 |  | 0 |  | 0 |
| 11 |  | FOAMING STABILITY SEQ3 |  | Milliliter |  | IS1448 (P67),ASTM D892 |  | 0 |  | 0 |  | 0 |
| 13 |  | FOAMING TENDENY SEQ2 |  | Milliliter |  | IS1448 (P67),ASTM D892 |  | - |  | - |  | 20 |
| 14 |  | FOAMING TENDENY SEQ3 |  | Milliliter |  | IS1448 (P67),ASTM D892 |  | - |  | - |  | 10 |
| 12 |  | FOAMING TENDENY SEQ1 |  | Milliliter |  | IS1448 (P67),ASTM D892 |  | - |  | - |  | 10 |
| 16 |  | RUST TEST SYNTHETIC SEA WATER |  | . |  | IS1448 (P96), ASTM D665 |  | P |  | P |  | P |

Note:

- The report refers only to the sample tested.

- The test report shall not be reproduced except in full without prior written approval of the Lab Incharge.

- This test report shall not be used in any advertising media or as evidence in the Court of Law without prior written consent of Laboratory.

- Test results reported are valid at the time of testing

- This is a system generated test report and hence does not require signature.

Reviewed and Authorized by: DALVI P Y(30044160)

Page No. :	5 of 6

*** END OF TEST REPORT ***