# HINDUSTAN PETROLEUM CORPORATION LIMITED

(A Government of India Enterprise)

QUALITY CONTROL LABORATORY

MAZGAON TERMINAL

LUBE PLANT, HAY BUNDER ROAD, MAZGAON MUMBAI,400033

# LABORATORY TEST REPORT

ENKLO 68 210 Ltr Drum(0254011)

Date

07/02/22

Laboratory Serial No.

FB 044

Sample Drawn By

QC OFFICER

JDE Serial No

1109251	Date Sample Drawn

11/01/22

Batch No / Lot No Work Order No

M1-22-A-176 909544

Date Received In Lab Date Tested

11/01/22

11/01/22

Tank /Kettle/Location

WHS

Particular of Sample	DRUM

Plant Code/ Name

14546	Mazgaon TML Lubes-(STP 0101)

Sampling Plan

IS 1447

Test Line Number

Test Description/ Characteristics

Specifications

Units	Test Method	Min	Max	Result Value

| 2 |  | ACIDITY TOTAL |  | mg KOH/g |  | IS1448 (P2), ASTM D974, D664 |  | - |  | 1.50 |  | .90 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 |  | APPEARANCE |  | . |  | VISUAL |  | B&C |  | B&C |  | B&C |
| 3 |  | DENSITY@29.5°C |  | gm/cc |  | IS1448(P16), ASTMD1298, D 4052 |  | .8000 |  | .9500 |  | .8601 |
| 4 |  | FLASH POINT,COC |  | °C |  | IS1448(P69), ASTM D92 |  | 210 |  | - |  | 240 |
| 5 |  | FOAM STABILITY ,SEQ 1 |  | Milliliter |  | IS1448(P67), ASTM D892 |  | 0 |  | 0 |  | 0 |
| 6 |  | FOAM STABILITY , SEQ 2 |  | Milliliter |  | IS1448(P67), ASTM D892 |  | 0 |  | 0 |  | 0 |
| 7 |  | FOAM STABILITY, SEQ 3 |  | Milliliter |  | IS1448(P67), ASTM D892 |  | 0 |  | 0 |  | 0 |
| 11 |  | KV @ 100 ° C |  | cSt |  | IS1448(P25), ASTM D445, D7042 |  | - |  | - |  | 9.462 |
| 10 |  | KV @ 40 ° C |  | cSt |  | IS1448(P25), ASTM D445, D7042 |  | 62.00 |  | 74.00 |  | 70.10 |
| 8 |  | POUR POINT ° C |  | °C |  | IS1448(P10), ASTM D97 |  | - |  | 0 |  | -6 |
| 12 |  | VISCOSITY INDEX (VI) |  | . |  | IS1448 (P56), ASTM D2270 |  | 90 |  | - |  | 113 |
| 9 |  | RUST TEST SYNTHETIC SEA WATER |  | . |  | IS 1448(P96),ASTM D665 |  | P |  | P |  | P |

Note:

- The report refers only to the sample tested.

- The test report shall not be reproduced except in full without prior written approval of the Lab Incharge.

- This test report shall not be used in any advertising media or as evidence in the Court of Law without prior written consent of Laboratory.

- This is a system generated test report and hence does not require signature.

Approved By : SHIRSAT NEETA VISHNU(38032820)

Page No. :	10 of 12

*** END OF TEST REPORT ***