| BHARAT PETROLEUM CORPORATION LIMITED (A Govt. of India Undertaking) QUALITY ASSURANCE LABORATORY : Budge Budge TC-7051 |  |  |  |
| --- | --- | --- | --- |
| TEST REPORT : MAK SHEROL BN |  |  |  |
| Issued to | PLANT MANAGER/CUSTOMER | Date | 12-10-2023 |
| Sample Id | 446404 | Date of Sampling | 04-10-2023 |
| Test Report Number | 23-64122 | Date of Receipt in Lab | 04-10-2023 |
| Type of Sample | Final | Date of Testing | 09-10-2023 |
| Source of Sample | BT7 | Reason for Testing | Batch Formation |
| Batch Number | B56245227/ |  |  |

| Sr.No. | Characteristics | Units | Test Method P of IS 1448/ASTM/ISO | Test Result |
| --- | --- | --- | --- | --- |
| 1 | Appearance | NA | VISUAL | Clear and Bright |
| 2 | Cast Iron Corrosion test | NA | IP - 125 | Pass |
| 3 | Colour-ASTM | NA | ASTM D - 1500 | 3 |
| 4 | Cracle | NA | SOP-10 | Negative |
| 5 | Density at 29.5°C | g/ml | ASTM D - 4052 | 0.8585 |
| 6 | Emulsion Test 20:1 - Cream | ML | P:98 | 0.00 |
| 7 | Emulsion Test 20:1 - Oil | ML | P:98 | 0.00 |
| 8 | Frothing Test 20:1 - Froth | ML | P:99 | 0.0 |
| 9 | Frothing Test 5:1 - Froth | ML | P:99 | 0.0 |
| REMARKS: 1.THE PRODUCT AS REPRESENTED BY THE SAMPLE MEETS THE SPECIFICATION OF MAK SHEROL BN w.r.t THE ABOVE TESTS CARRIED OUT AS PER INTERNAL SPECIFICATION. Notes: - The result relates to the sample tested. - The certificate shall not be reproduced wholly or in part without prior written consent of the laboratory - This certificate shall not be used in any advertising media or as evidence in the court of law without written consent of laboratory NA - Not Applicable - Latest version of test methods are used as per latest specification |  |  |  |  |

| Authorised Signatory | sharmaganeshraj |
| --- | --- |
| Note : This document has been generated electronically and is valid without signature. |  |

*** End of Test Report***

# Page 1 of 1